A facile synthesis of montmorillonite supported CdAl2O4 nanocomposites with photocatalytic and hydrophobic properties

Fig. SI 1. XRD pattern of 9% wt Montmorillonite clay supported CdAl2O4

3.35 eV

0

4

8

12

0

1

2

3

4

5

6

7

Photon Energy (eV)

(ahγ)2

2.89 eV

(a)

(b)

Fig. SI 2. Tauc energy plot of (a) Undoped CdAl2O4 and (b) 9% wt Montmorillonite clay supported CdAl2O4

Fig. SI 3. EDAX image of Montmorillonite clay

0

20

40

60

80

100

0

15

30

45

60

% of Rh-B dye remaining

Time (min)

(f)

(c)

(b)

(a)

(d)

(e)

Fig. SI 4. Photodegradability of Rh–B with different catalysts: (a) Dark (b), Catalyst without light (c) Montmorillonite clay (d) Undoped CdAl2O4 (e) 3% wt MMT/CdAl2O4 and (f) 5% wt MMT/CdAl2O4, dye concentration = 3 × 10−4 M, catalyst suspended = 3 g L−1, pH = 7, airflow rate = 8.1 mL s−1, IUV = 1.381 × 10−6 einstein L−1 s−1, irradiation time =45 min.